Sapphire and oxide eutectic fibers grown by the EFG technique

Dmitry Stryukov*, Kurlov Vladimir

Institute of Solid State Physics Russian Academy of Sciences,

2 Academician Ossipyan str., 142432 Chernogolovka, Moscow District, Russia

*email: stryukov@issp.ac.ru

Single crystalline sapphire has a high melting point, chemical inertness, impressive hardness, radiation and mechanical strength, high thermal shock resistance, and thermal conductivity. Sapphire also has a high refractive index and a broad transmission band spanning the UV, visible, IR, THz, and microwave bands [1]. Such unique combination of physical and chemical properties makes sapphire an attractive material for various applications. Some oxide eutectic ceramics also are attracting attention as candidates for next-generation high-temperature applications [2].

High-quality single-crystalline (sapphire, yttrium-aluminum garnet) as well as eutectic double garnet-containing (Al2O3-Y3Al5O12, Al2O3-Er3Al5O12,) and perovskite-containing (Al2O3-GdAlO3) fibers with diameters from 150 μm was grown by multi-crystal growth process from the melt [3]. An automated control system for the process of growing oxide fibers from the melt has been developed [4]. A system of fiber diameter stabilization was developed, which allowed to reduce the surface roughness of the grown fibers to tens of nanometers [5].

It can be useful for development of various optical fiber sensors for use in chemically aggressive and high-temperature environments. In addition, some perovskite eutectics contain rod-like structure with single crystalline phases, which makes them attractive for photonic applications.

[1] Kurlov V. N. Sapphire: Properties, Growth, and Applications. In book: Reference Module in Materials Science and Materials Engineering, Oxford: Elsevier, 2016. pp. 1-11. DOI: 10.1016/B978-0-12-803581-8.03681-X

[2] Llorca J., Orera V. M. Directionally solidified eutectic ceramic oxides. Prog Mater Sci. 2006; 51: 711–809.

[3] Kurlov V.N., Stryukov D. O., Shikunova I. A. “Growth of sapphire and oxide eutectic fibers by the EFG technique” - Journal of Physics: Conference Series 673 (2016) 012017

[4] S.N. Rossolenko, G.M. Katyba, I.N. Dolganova, I.A. Shikunova, D.O. Stryukov, K.I. Zaytsev, V.N. Kurlov, Numerical Analysis of Liquid Menisci in the EFG Technique. Ch.3 in book: Crystal Growth, IntechOpen, London, 2019, pp. 1–21, ISBN: 978-953-51-6326-8.

[5] Kurlov V.N., Shikunova I.A., and Stryukov D.O., RF Patent 2552436, 2015.